## Slide 1: 2 Level rate equations

## Slide 2: Modeling an EDFA
Assume pump transition undergoes non-radiative decay immediately to the metastable state → can model as a two-level system:
If the → will reach steady state
Pump term
Signal term
Spontaneous decay
Set and solve for

## Slide 3: Rate Equations
where:
Need to know:
Absorption cross-section (m2)
Emission cross-section (m2)
Fiber core size
Excited state lifetime (well known from literature 10 ms)
The gain coefficient is:
Steady state
cross-sections:
= small signal absorption is known

## Slide 4: 2W pump, 2 m of ER 80
Unphysically high conversion efficiency!
Used: 0.7 dB insertion loss, 0.2 dB splicing loss
Since seed power is quite high, this likely isn’t due to unaccounted ASE?
So, the next step to try is to account for excited state absorption, since after all green fluorescence is always observed.

## Slide 5: Accounting for excited state absorption

## Slide 6: ESA for both pump and signal 5-levels
You need to include lifetimes to “close” the circuit if you want to apply steady state (i.e. electron number needs to be conserved)
You can isolate population to the laser excited state (2), pump level (3), and pump excited state (5) which is responsible for the green fluorescence.
  Done by making the lifetime of (4) much smaller than the others (e.g. ns)
Yu. O. Barmenkov, et al., Journal of Applied Physics 106, 083108 (2009).
Solve for n1 n2 n3 n4 n5 in terms of ntot = n1 + n2 + n3 + n4 + n5
Computed in Mathematica and then copied to Python using Sympy

## Slide 7: 2W pump, 2 m of ER 80
Not perfect, but much more realistic power evolution, maybe actually a little too lossy.
Used: 0.7 dB insertion loss, 0.2 dB splicing loss
Better match to experiment can be achieved by varying 5-level parameters, although the ones obtained from Barmenkov et al. are not too bad. Their numbers are similar to other older papers.

## Slide 8: 2W pump, 2 m of ER 80
Backward pumping also matches experiment better.
Used: 0.7 dB insertion loss, 0.2 dB splicing loss
Calculated using shooting method

## Slide 9: Some things to note for amplifiers

## Slide 10: Combining EDF’s for more conversion efficiency
ER 80 4/125 + 8/125 is better than 4/125 on it’s own, and helps with gain narrowing
Used 0.7 dB splicing loss between the 4 and 8 micron cores
Power is achievable with just the anomalous, but the spectrum can be optimized by combining the two
ER 80 4/125
ER 80 4/125 + ER 80 8/125
ER 80 4/125 + ER 80 8/125

## Slide 11
Extending further from the last slide:
The order of normal and anomalous EDF gives different results
You want the higher power to go through the anomalous section

## Slide 12: Figure 9 cavity

## Slide 13: Setup
While loop:
Splitter splits envelope 50/50
Clockwise arm:
  gain section, propagated with the pump
  phase bias
Counter-Clockwise arm:
  Phase bias
  Gain section, propagated against the pump
The sum of the two fields: is sent to the straight section, which means the output coupler takes out
I haven’t checked this, but most of the difference in nonlinear phase shift should be acquired by the difference in forward vs backward seeding. So, I haven’t tested placing the gain section closer to center vs. one side of the loop
Simultaneous forward and backward seeding is calculated using shooting method
With pump in EDF
Against pump in EDF
Using:

## Slide 14: Looking for stability
Run simulation until output spectrum doesn’t differ from the previous by more than some threshold
Seed with a 1 mW 2ps pulse. (So, kind of skip to the middle where you already have quasi-CW?)
If loop counts exceed 500, then cavity is deemed unstable.
Output spectrum for 200 MHz, 11 cm straight section, 4 ps/nm/km round trip dispersion, 500 mW pump
not
stable
Being too normal doesn’t work. However, too anomalous is not good either as a higher pump current is needed to reach the same bandwidth.
stable

## Slide 15: 200 MHz
200 MHz, 4.5 ps/nm/km round trip
11 cm straight arm
  accounting for: 0.7 dB insertion loss and 0.7 dB splicing loss
400 mW pump
450 mW pump
Output coupler:
Reflected back to cavity:

## Slide 16: 100 MHz
100 MHz, 3.5 ps/nm/km round trip
15 cm straight arm
  accounting for: 0.7 dB insertion loss and 0.7 dB splicing loss
Output coupler:
Reflected back to cavity:
60 mW pump
75 mW pump

## Slide 17: Length of straight section is important
15 cm straight section @ 100 MHz
I can’t quite pin down the effect of elongating the straight section
I think it has a similar effect as pushing the cavity more anomalous, even if the round-trip dispersion is kept the same?
Each simulation takes 5 – 7 min, so I haven’t tested parameters thoroughly, but at 100 MHz I think I can push the straight section to around 30 cm. Whereas, for 200 MHz, I have a hard time reaching stability with any straight section longer than 11 cm
  This is different than what I was doing experimentally, where I thought only the total round trip dispersion mattered. I think it turns out different lengths of straight section has a big effect.
20 cm straight section @ 100 MHz
30 cm straight section @ 100 MHz

## Slide 18: 200 MHz with ER 110 normal + ER 80 anomalous
Typically when you mode-lock, I think you start out with the broadest supported spectrum with the given dispersion, and then narrow some as you tune down the pump current. The goal is to push the broadest spectra below 500 mW pump in the EDF.
Propagation with the pump needs to have higher pulse energy in the normal section, so the order of normal edf and anomalous edf matters. Reversing the order causes the pulse to never stabilize.
There should be an optimal length of anomalous edf?:
  50 and 45 cm total of anomalous + normal edf doesn’t seem to have a dispersion regime that gives stable pulses…?
  40 cm total of anomalous + normal edf seems to work better than just using normal edf. Using 0.7 dB splicing loss between anomalous and normal edf, but no splicing loss between anomalous and pm1550
    Required round trip dispersion is more anomalous compared to using only normal edf
6 ps/nm/km at 400 mW pump, 200 MHz
28.3 cm of normal edf + 11.6 cm of anomalous edf
with pump in edf
against pump in edf